Flexible 1D photonic crystals and active planar waveguides fabricated by RF-Sputtering

G. Zanetti1,2 , A. Carlotto1,3, L.T. N. Tran1,4,5, A. Szczurek1, B. Babiarczuk6, O. Sayginer7, 
S. Varas1, A. Vinante1,J. Krzak6, O. S. Bursi8,1, D. Zonta8,1, A. Lukowiak9, G. C. Righini10, 
M. Ferrari1, V. M. Sglavo2, M. Bonomo11, S. Galliano11, C. Barolo11, S. M. Pietralunga3, 
A. Chiasera1

1IFN-CNR, CSMFO Lab and FBK Photonics Unit, Trento; 2Department of Industrial Engineering, University of Trento; 3IFN-CNR, Milano; 4Dept. of Physics, Politecnico di Milano; 5Dept. of Materials Technology, Faculty of Applied Sciences, HCMC University of Technology and Education; 6Dept. of Mechanics, Materials and Biomedical Engineering, Wroclaw University of Science and Technology; 7Department of Mechanical Engineering, Temple University; 8DICAM, University of Trento; 9ILTSR PAS, Wroclaw; 10IFAC-CNR, MiPLab; 11Department of Chemistry, NIS Interdepartmental Centre and INSTM Reference Centre,University of Turin;
e-mail: chiasera@fbk.eu

We present the RF-Sputtering fabrication of flexible 1D photonic crystals and active Er3+ planar waveguides. The structures were deposited on ultrathin flexible glass and show very valuable results in terms of both optical and mechanical properties, making RF-Sputtering a promising and scalable technique to fabricate flexible photonic devices [1,2]. In addition, we report about the design and performance of flexible 1D photonic crystals fabricated by RF-Sputtering multi-layered deposition on a flexible thermosetting polymer, showing comparable results with respect to the ones of the film deposited on glass. Experimental spectroscopic analysis of the performance is provided under various bending configurations, and it is in accordance with numerical simulation and sets the conditions for reliably operating the photonic device.

Acknowledgements:

This research is supported by the projects: FESR-PON 2014-2020 BEST4U ARS01_00519; CNR-PAS “Flexible Photonics” (2020-2022); NAWA PPN/IWA/2018/1/00104; MIUR-‘Departments of Excellence’ L 232/2016; ERC-H2020 PAIDEIA GA 816313; “nuovi Concetti, mAteriali e tecnologie per l’iNtegrazione del fotoVoltAico negli edifici in uno scenario di generazione diffuSa” CANVAS, LEMAQUME-QuantERA,  and NAWA-MAECI Canaletto (2022-2023).

References:

[1] G. Zanetti, et.al., Optical Materials X (2023); doi: 10.1016/j.omx.2023.100241.

[2] A.Carlotto, et.al., Ceramics International, (2023); doi:10.1016/j.ceramint.2023.03.012