## Slide 1: Toward transparent and colorless Dye-Sensitized Solar Cells for non-intrusive BIPV
S. Galliano,a A.Y. Segura Zarate,a M. Rubes,a M. Bokan,a N. Barbero,a,b M. Bonomo,a R. Borrelli,c
W. Naim,d F. Grifoni,d F. Matteocci,e P. Chotard,f S. Ceurstemont,f F. Barath,f A. Di Carlo,e
F. Sauvage,d and C. Baroloa,b,g
a Dipartimento di Chimica, NIS Interdepartmental and INSTM Reference Centre, Università degli Studi di Torino, Torino, Italy
b Istituto di Scienza, Tecnologia e Sostenibilita ` per lo sviluppo dei Materiali Ceramici (ISSMC-CNR), Faenza (RA), Italy
c Dipartimento di Scienze Agrarie Forestali e Alimentari, Università degli Studi di Torino, Grugliasco (TO), Italy
d CNRS, Laboratoire de réactivité et Chimie du Solide (LRCS), Université Picardie Jules Verne, Amiens, France
e CHOSE, Dipartimento di Ingegneria Elettronica, Università di Roma Tor Vergata, Roma, Italy
f G-LYTE SAS, Amiens, France
g ICxT Interdepartmental Centre, Università degli Studi di Torino, Torino, Italy
Milano, 22-23/06/2023

## Slide 2
Façades
Rooftops
Windows
Building Integrated Photovoltaics
Agrivoltaics

## Slide 3
Façades
Rooftops
Windows
Building Integrated Photovoltaics
Agrivoltaics
Replacing windows with
transparent and colorless solar cells
Transparent PVs can reduce visual pollution without reciding from original design

## Slide 4
50% solar irradiance falls in the NIR
Only molecular-based devices can afford selective NIR-conversion
International Commission on Illumination. Colorimetry. (CIE); 2004.
a
b
Color purity
Wavelenght selective transparent photovoltaics
F. Grifoni, et al. Adv. Energy Mater. 2021.
Figures of merit
Avarage Visible Transmittance =
High CRI
Low CRI
Color Renderind Index
CRI>90 excellent quality
x,y coordinates in CIE 1931
Light Utilization Efficency = PCE x AVT

## Slide 5
Luminescent Solar Concentrators
Organic Solar Cells
Lower transparency (AVT=64%)
Higher efficiency (PCE=4%)
High transparency (AVT=88.3%)
Low efficiency (PCE=0.4%)
Traverse, C. J. et al. Nat. Energy 2, 849–860 (2017).
Chen, C. et al. ACS Nano (2012).
Only molecular-based devices can afford selective NIR-conversion
50% solar irradiance falls in the NIR
Wavelenght selective transparent Photovoltaics
F. Grifoni, et al. Adv. Energy Mater. 2021.
Figures of merit
Avarage Visible Transmittance =
High CRI
Low CRI
Color Renderind Index
CRI>90 excellent quality
x,y coordinates in CIE 1931
Light Utilization Efficency = PCE x AVT

## Slide 6
Chen, C. et al. ACS Nano (2012).
Luminescent Solar Concentrators
Organic Solar Cells
Lower transparency (AVT=64%)
Higher efficiency (PCE=4%)
High transparency (AVT=88.3%)
Low efficiency (PCE=0.4%)
Traverse, C. J. et al. Nat. Energy 2, 849–860 (2017).
NIR Dye-Sensitized Solar Cells
Filling the gap
Only molecular-based devices can afford selective NIR-conversion
F. Grifoni, et al. Adv. Energy Mater. 2021.
50% solar irradiance falls in the NIR
Figures of merit
Avarage Visible Transmittance =
High CRI
Low CRI
Color Renderind Index
CRI>90 excellent quality
x,y coordinates in CIE 1931
Light Utilization Efficency = PCE x AVT
Wavelenght selective transparent Photovoltaics

## Slide 7
Dye-Sensitized Solar Cells
Simple preparation procedure
Low production cost
Work with weak/diffuse light
Efficiency 14% outdoor, >30% indoor
Transparency, flexibility, …
Material recyclability

## Slide 8
Grant agreement 826013
SC3-RES-2-2018
NIR
NIR-dye-sensitized solar cells
Development of NIR dyes (> 700 nm)
Development of transparent redox mediator
Development of transparent back-contact
Objectives 75 % AVT – 8 % PCE
Achieving 55% AVT - 14% PCE
4 terminal
Tandem cells and modules
UV-perovskite solar cells
UV
Development of UV perovskite absorber (< 450 nm)
Development of transparent HTM
Development of transparent contacts
Objectives 75 % AVT - 6 % PCE
IMPRESSIVE Project
courtesy of Frederic Sauvage
Ground-breaking tandem of transparent dye-sensitized and perovskite solar cells
Project Coordinator: Prof. F. SAUVAGE (Research Director at CNRS)
https://impressive-h2020.eu

## Slide 9
https://doi.org/10.1002/aenm.202101598
Transparent electrodes
Transparent redox couples
NIR-selective dyes
Development on NIR cell: DSSC cell with AVT ≥ 75% resulting in a high PCE

## Slide 10
Polymethine-based dyes: far RED to NIR
Quaternization reactions in order to increase the acidity of the methyl group
R = H, CH2, C4H9, C8H17, C10H21, C16H24, Alk-X
DOE OPTIMIZATION
Croconine VG25
Squaraine VG10
Cyanine VG20

## Slide 11
VG20-C16
R=-C16H33
https://impressive-h2020.eu/
BG: 1,45 eV
HOMO: -5,27 eV
LUMO: -3,82 eV
AVT 70%
CRI 92
Naim, W. et al. JACS Au 2021, 1, 409−426

## Slide 12
https://impressive-h2020.eu/
Grifoni F. et al. Manuscript in preparation
Low-temperature sensitization approach affords reaching 3.1 % PCE (with scattering layer)
Polysulfide with have negligible absorbance in the Vis in ACN
confirmed by MS
TMA+
Thiolate
Electrolyte | Voc (mV) | Jsc (mA/cm²) | Fill factor (%) | PCE (%)
ESI | 359 | 11.2 | 58 | 2.4
EI | 402 | 11.5 | 58 | 2.6

## Slide 13: Some conclusions and more perspectives
Demonstrated the feasbility of selective NIR-DSSC with high transparency and color neutrality
We need to do better to overcame aggregation as a limitation for both performances and aesthetics
Obtained AVT=80%, CRI=96 with promising thiolate-based electrolyte.
Optimized the thickness for the best Light Utilization Efficiency
Technology completely non-intrusive with first modules
Still a lot of work to do…
4T-tandem UV-PSC/NIR-DSSC
Bonomo et al. Manuscript in preparation
New Dyes

## Slide 14
λmax from 643 to 827 nm
Far-Red / NIR polymethine dyes

## Slide 15
Evolution of Polymethine dyes
New synthesized compounds to improve the
chemical-physical properties of the selected dyes
substitutions on the linker chain
between the benzo[e]indole moieties
Starting from C2 to C8 alkyl chains and eventually synthetic strategies for C16 alkyl chains
cyanine dyes without carboxylate groups (C2-8-16) and
with –COOH (C2-C8) anchoring group in the linker chain
between the benzo[e]indole moieties
(VG40 serie)
Unpublished results

## Slide 16
16
 | E1/2/ V vs Ag/AgCl | E1/2/ V vs Fc/Fc+ | HOMO / eV | E0/0 / eV | LUMO / eV
VG20 | 0.660 | 0.150 | -5.25 | 1.30 | - 3.95
VG30 | 0.840 | 0.330 | -5.43 | 1.55 | - 3.88
VG39 | 0.696 | 0.186 | -5.29 | 1,60 | -3.69
I- / I3-
BG = 1,30 BG = 1,55 BG = 1,60
VG20 VG30 VG39
+ 0.89
- 0.71

## Slide 17
17
Unpublished results
 | E1/2/ V vs Ag/AgCl | E1/2/ V vs Fc/Fc+ | HOMO / eV | E0/0 / eV | LUMO / eV
VG20 | 0.660 | 0.150 | -5.25 | 1.30 | - 3.95
VG30 | 0.840 | 0.330 | -5.43 | 1.55 | - 3.88
VG47 | 0.672 | 0.162 | -5.26 | 1.51 | - 3.75
Unpublished results
VG20 VG30 VG47
B.G.
1.30
B.G.
1.55
B.G.
1.51

## Slide 18
https://impressive-h2020.eu/
Grifoni F. et al. Manuscript in preparation
Dye | JSC (mA/cm2) | VOC (mV) | η (%)
VG20-C16 | 13.0 | 375 | 3.1
VG20-C2 | 7.8 | 415 | 2.2
VG28-C2 | 8.1 | 275 | 1.4
VG29-C2 | 9.1 | 422 | 2.4
VG30-C2 | 7.2 | 340 | 1.9
VG47-C2 | 1.3 | 328 | 0.32

## Slide 19: Some conclusions and more perspectives
Demonstrated the feasbility of selective NIR-DSSC with high transparency and color neutrality
We need to do better to overcame aggregation as a limitation for both performances and aesthetics
Obtained AVT=80%, CRI=96 with promising thiolate-based electrolyte.
Optimized the thickness for the best Light Utilization Efficiency
Technology completely non-intrusive with first modules
Still a lot of work to do…
4T-tandem UV-PSC/NIR-DSSC
Bonomo et al. Manuscript in preparation
New Dyes

## Slide 20
https://impressive-h2020.eu/
Bonomo et al. Manuscript in preparation
NIR-DSSC
UV-PSC
4T-tandem UV-PSC/NIR-DSSC
3.0% 3.0% 3.6%

## Slide 21
Grant agreement 826013
Grant agreement 826013
Thanks for your kind attention!
Staff: G. Viscardi, C. Barolo, N. Barbero,
P. Quagliotto, A. Fin, M. Bonomo,
I. Benesperi, F. Cardano
PostDoc: M. Bokan, C. Pontremoli, S. Neirotti, D. Pasculli
PhD: D. Alencar, A. Segura, B. Centrella,
M. Rubes, B. Charrier, M. Franzini, D. Dereje, V. Maruzzo, G. Viada, D. Gallo
A. Di Carlo, F. Matteocci
R. Borrelli
F. Sauvage, W. Naim, F. Grifoni
F. Barath,
P. Chotard,
S. Ceurstemont