Photocatalytic Transformations of 1H-Benzotriazole and Benzotriazole Derivates

Marco Minella1, Elisa De Laurentiis1, Francesco Pellegrino1,2, Marco Prozzi1, Federica Dal Bello3, Valter Maurino1,2* and Claudio Minero1

1	Chemistry Department and NIS Interdepartmental Centre, University of Torino, Via P. Giuria 5, Turin, 10125, Italy.

2	JointLAB UniTo-ITT Automotive, Via Quarello 15/A, 10135 – Torino, Italy

3	Department of Molecular Biotechnology and Health Sciences, University of Torino, Via P. Giuria 5, Turin, 10125, Italy.

*	Correspondence: valter.maurino@unito.it; Tel.: +39 011 6705218; Web: http://www.environmentalchemistry.unito.it

Supplementary Materials

Table S1. Main chemical and physical characteristics of the three compounds considered

| Name | 1H-benzotriazole | Tolyltriazole | Tinuvin P |
| --- | --- | --- | --- |
| Chemical Formula | C6H5N3 | C7H7N3 | C13H11N3O |
| Molecular Mass, u | 119.05 | 133.06 | 225.09 |
| Solubility in water (25°C) (around neutrality) | 28 g dm-3 | 7 g dm-3 | < 0.01 g dm-3 (soluble in basic media) |
| pKa | 8.6 | 8.8 | / |
| LogKow (octanol-water) | 1.23 | 1.89 | 4.31 |

Table S2. Initial degradation rates for the photocatalytic degradation of 1H-benzotriazole and tolyltriazole 1(10–4 M at different pHs (TiO2 P25 0.5 g dm-3).  The error bars are computed as the fitting error of the experimental profiles obtained from the replicates.

|  | Degradation rate, mM min-1 |
| --- | --- |
|  | 1H-benzotriazole | Tolyltriazole |
| pH 3 | (2.27(0.09)(10–2 | (2.0(0.1)(10–2 |
| pH 6 | (1.2(0.1)(10–2 | (2.00(0.08)(10–2 |
| pH 11 | (3.88(0.05)(10–2 | (2.11(0.09)(10–2 |

Figure S1. Non Purgeable Organic Carbon (NPOC) evolution during the photocatalytic degradation of 1H-benzotriazole and tolyltriazole at pH 3 (Conditions: BTz and TTz nominal initial concentration 1(10–3 M; TiO2 P25 0.5 g dm–3).

Figure S2. ESI–HRMS chromatograms of a 1H–benzotriazole suspension irradiated under photocatalytic conditions (conditions: initial nominal concentration 5.0(10–4 M, irradiation time 15 minutes, pH 3). Lower trace: total ion current (TIC) chromatogram, note the only presence of the peak related to BTz (tr = 8.6 minutes); upper trace: extracted chromatogram (XIC) related to the m/z equal to 136 and 152 (mono and bihydroxylated BTz intermediates).

Figure S3. ESI–HRMS spectra of 1H-benzotriazole. Note the signal at m/z= 120.0535 corresponds to the accurate mass, within the experimental error, of protonated BTz (C6N3H5, m/z= 120.056).

Figure S4. ESI–MS2 spectra of 1H–benzotriazole (precursor ion: 120 m/z). Note the formation of a product ion with m/z 92.047 that corresponds to the loss of a N2 molecule (120.053–92.047= 28.006, accurate mass of molecular nitrogen). The loss of a HCN molecule from the product ion with m/z 92.047 generates the fragment with m/z 65.037 (92.047 – 65.037 = 27.010, the accurate mass of a HCN molecule is 27.0110).

Figure S5. ESI–HRMS chromatograms of a tolyltriazole suspension irradiated under photocatalytic conditions (conditions: initial nominal concentration 1.0(10–4 M, irradiation time 30 minutes, pH 6). a) XIC for m/z 134.072, note the only presence of the peak related to TTz (tr = 14.22 minutes); b) XIC for m/z 150.067 (hydroxylated TTz isomers mass, note the presence of at least four isomers; c) XIC for m/z 166.062 (bihydroxylated TTz isomers mass), note the presence of at least three different isomers.

Figure S6. a) ESI–HRMS spectra of the tolyltriazole peak. Note the signal at m/z= 134.138 that corresponds to the accurate mass of protonated TTz (C7N3H8, m/z= 134.072). b) ESI–MS2 spectra of tolyltriazole (precursor ion: 134 m/z). Note the formation of a product ion with m/z 106.117 that corresponds to the loss of a N2 molecule (134.1381–106.1176 = 28.0205, the accurate mass of molecular nitrogen is 28.006). The loss of a HCN molecule from the product ion with m/z 106.117 generates another product ion with m/z 79.093 (106.118 – 79.093 = 27.025, the exact mass of a HCN molecule is 27.011).

Figure S7. a) ESI–HRMS spectra of the peak at retention time = 13.49 min. Note the signal at m/z= 150.1411 that corresponds to the accurate mass of a monohydroxylated TTz isomer (C7N3OH8, m/z= 150.067). b) ESI–MS2 spectra of the same monohydroxylated tolyltriazole isomer (precursor ion: 150 m/z). Note the formation of a product ion with m/z 132.167 that corresponds to the loss of a H2O molecule (150.141–132.167 = 17.974, the accurate mass of water is 18.020). The fragment with m/z 122.121 was formed after the loss of a N2 molecule from the precursor ion (150.141-122.121=28.030, exact mass of N2 28.006). The loss of CO from the 122.121 ion generates the product ion with m/z equal to 94.112 (122.121 – 94.112 = 28.009, the accurate mass of CO is 27.995). The product ion with m/z 77.076 is formed from the successive loss of N2 and HCN from the ion with m/z equal to 132.167 (132.167–77.076=55.091, the sum of the accurate masses of N2 and HCN is 55.017).

Figure S8. ESI–HRMS chromatograms of a Tinuvin P suspension irradiated under photocatalytic conditions (conditions: initial nominal concentration 1.0(10–4 M, irradiation time 60 minutes, pH 3, solvent acetonitrile:water 90:10). a) XIC for m/z 226.098 (m/z protonated Tinuvin P, retention time 19.75 minutes); b) XIC for m/z 242.093 (hydroxylated TP isomers mass); c) XIC for m/z 258.088 (bihydroxylated TP isomers mass); d) XIC for m/z 120 (1H-benzotriazole).

Figure S9. ESI–HRMS spectra of the peak at retention time a) 9.51 minutes and b) 10.45 minutes. Note the signals at m/z= 242.093 and m/z= 258.088 that correspond to the accurate mass of a monohydroxylated TP isomer (C13H12N3O2, m/z= 242.093) and of a bihydroxylated TP isomer (C13H12N3O3, m/z= 258.088) respectively. Figure S10. ESI–MS2 spectra of a) a monohydroxylated Tinuvin P isomer (precursor ion: 242 m/z); b) a bihydroxylated Tinuvin P isomer (precursor ion: 258 m/z). Note in each case the presence of a product ion with m/z 120.056 that corresponds to the mass of 1H-benzotriazole (C6N3H5, m/z = 120.056). Figure S11. Tinuvin P and 1H-benzotriazole concentration time profile during the Tinuvin P photodegradation at pH 3 (Conditions: Tinuvin P initial concentration 1(10-4 M, Solvent CH3CN/H2O 90/10, TiO2 Degussa P25 0.5 g dm-3)